| # EQUIVALENT TO UNICELL |  |  |
| --- | --- | --- |
| Height | 800 1000mm |  |
| Equivalent to DCE Our Ref | 6339 9000 6439 9000 DRCELL800P 1000P |  |
| Flange | 500 x 95mm |  |
| Bottom | 480 x 75mm |  |
| Gasket | None |  |
| Pleat number | 2 x 38 |  |
| Pleat depth | 35mm |  |
| Filtration area | 4m2 5m2 |  |
| Pleat spacing | Uniform pleat spacing on both inside and outside diameters for maximum life with minimum airflow restriction. |  |
| Filter media | A 240g/m2 Polyester. 0.62mm thickness 105-150 l/m2/sec Air Permeability |  |
| Inner sleeve | None |  |
| Outer sleeve | None |  |
| End caps | PU |  |
| Pleat/end cap bonding |  |  |
| Filter class | F9 |  |
| Operating temperature | 120ºC |  |